## Slide 1: Characterization techniques applied to Carbon Nanowires
Angel Manuel Villalba Rodríguez <A00828035@itesm.mx>
Constanza Alvarez Lopez <A00829469@itesm.mx>
Antonio Osamu Katagiri Tanaka <osamu.katagiri@exatec.tec.mx>
Tuesday, 19 May 2020

## Slide 2: Agenda
Introduction : <5min
Characterization Techniques : ~20min
  Rheometry
  Scanning Electron Microscopy (SEM)
  Raman Spectroscopy
  Thermogravimetric analysis (TGA)
  4-Wire Kelvin
Conclusions : <5min

## Slide 3: Introduction: Project overview
To design polymer solutions that can be electrospun by NFES, photopolymerized, and then pyrolyzed into conductive carbon nano-wires.
Polymer Solution
Polymeric micro-fibers
Carbon nano-fibers
Near-Field Electrospinning & Photopolymerization
Pyrolysis and Carbonization
Rheometry
SEM
Raman Spec.
TGA
4-Wire Kelvin
SEM
Fabrication Process
Product
Characterization Technique

## Slide 4: Charc. Techniques: Rheometry (instrumentation)
Discovery Hybrid Rheometers – TA Instruments, (n.d.). https://www.tainstruments.com/products/rheology/discovery-hybrid-rheometers/ (accessed 18 May 2020).
A.B. Metzner, Rheology. Theory and Applications., J. Am. Chem. Soc. 81 (1959) 1520–1521. https://doi.org/10.1021/ja01515a070.
Measured Parameter | Calculated Parameter
Torque Angular displacement Angular velocity | Stress Strain Shear rate
Notes: •Torque is a measure of how much a force acting on an object causes that object to rotate
•Shear stress is calculated from the torque and geometry stress constant
---
•Angular displacement is the angle, in radians, through which an object moves on a circular path
•Strain is a measure of deformation representing the angular displacement relative to a reference length
---
•Angular velocity is the change in angular displacement per unit time of measurement
•Shear rate is calculated from the angular velocity and geometry strain constant
---
Constants are geometry type and sample size dependent.
---
•The Modulus tells how much a material will deform elastically when you apply a certain amount of stress
•Viscosity tells how fast the material will flow

## Slide 5: Charc. Techniques: Rheometry (process parameters)
A.B. Metzner, Rheology. Theory and Applications., J. Am. Chem. Soc. 81 (1959) 1520–1521. https://doi.org/10.1021/ja01515a070.
Geometry options:
Important rheometer parameters:
Torque range
Angular Resolution
Angular Velocity Range
Frequency Range
Concentric Cylinders
Cone and Plate
Parallel Plate
Torsion Rectangular
Very Low Viscosity
Solids
Notes: •In general, lower viscosity use larger diameter or larger contact area and higher viscosity or more solid-like smaller diameter

## Slide 6: Charc. Techniques: Rheometry (Carreau-Yasuda Model)
Osswald, T., Rudolph, N., Osswald, T., & Rudolph, N. (2014). Generalized Newtonian Fluid (GNF) Models. Polymer Rheology, 59–99. https://doi.org/10.3139/9781569905234.003

## Slide 7: Charc. Techniques: Rheometry (Example results)
Notes: Zero shear and infinite shear viscosities of 5 PEO and SU-8 solutions at different concentrations.

## Slide 8: Charc. Techniques: Raman Spectroscopy
Collect knowledge about molecular information and crystalline structures. A laser irradiate the sample with monochromatic radiation, with excitations in the UV, visible and near-IR spectral region (785-1064nm). The irradiation generates a Raman spectrum of scattered light.
C. Eid, A. Brioude, V. Salles, J.-C. Plenet, R. Asmar, Y. Monteil, R. Khoury, A. Khoury, P. Miele, Iron-based 1D nanostructures by electrospinning process, Nanotechnology. 21 (2010) 125701. https://doi.org/10.1088/0957-4484/21/12/125701.
Expectation is to find two bands (marked D and G in the figure), centered about 1360 and 1594 to confirm the presence of graphitic carbon in the nanofibers.

## Slide 9: Charc. Techniques: 4-Wire Kelvin
<content> <key concept>
Notes: https://www.allaboutcircuits.com/textbook/direct-current/chpt-8/kelvin-resistance-measurement/

## Slide 10: Charc. Techniques: Scanning Electron Microscopy (SEM)
A beam of electrons scans across the material surface, producing high-energy back-scattered electrons and low-energy secondary electrons. The back-scattered electrons provides a physical image of the sample surface.
Coating may be not necessary, depending on the carbon nanowire chirality and conductivity.
Fiber diameter before pyrolysis
Fiber diameter after pyrolysis
B. Cárdenas, Advanced Manufacturing Techniques for the Fabrication and Surface Modification of Carbon Nanowires, (2017) 160.
Notes: Porosity,
Surface distribution, and
Fiber morphology

## Slide 11: Charc. Techniques: Thermogravimetric analysis
<content> <key concept>

## Slide 12: Conclusions:
<Conclusion A>
<Conclusion B>

## Slide 14: References:
<reference A>
<reference B>