## Slide 1: Surface Energy and Thermodynamic Potentials*
February 17th, 2020
* Based on a presentation from the author´s book

## Slide 2: Question…
Is it the same surface energy and surface tension?

## Slide 3: Percentage of surface atoms changes with cluster diameter

## Slide 4
For 1 g of Sodium Chloride, the original 1 g cube is successively divided into smaller cubes.

## Slide 5: Comments:
Due to the vast surface area, all nanostructured materials possess a huge surface energy and, thus are thermodynamically unstable or metastable.
Goal: to overcome the surface energy, and to prevent the nanomaterials from growth in size, driven by the reduction of overall surface energy.

## Slide 6
Surface Energy
Definition: energy required (or produced) to create a unit area of a new surface, therefore,
γ = (∂G/ ∂A)ni, T, P
G: Gibs free energy of the surface
A: Surface area of the particles
Surface area can be increased by cutting a particle into two halves. The molecules of the newly created surface possess fewer nearest neighbors or coordination numbers, and thus have dangling or unsatisfied bonds. Due to the dangling bonds on the surface, surface atoms or molecules are under an inwardly directed force and the bond distance between molecules and the sub-surface molecules becomes smaller. An extra force or energy is required to pull the surface to its original positions.

## Slide 7
Surface Energy
This energy is defined as surface energy, γ
        γ = Nb ε ρa /2 = (∂G/ ∂A)ni, T, P
Nb: number of broken bonds
ε: bond strength
ρa = number of atoms or molecules per unit surface area density
The above equation is very crude model and does not account for interactions between higher order neighbors.
gla

## Slide 9
Surface Energy
For FCC structure with lattice constant a, each atom will have a coordination number 12, and each atom on the surface {100} has 4 broken bonds, on {110} 5 broken bonds and on {111} 3 broken bonds. Therefore,
g = Nb ε ρa /2
γ{100} = 2/a2．4．ε．1/2
γ{110} = 2/20.5a2．5．ε．1/2
γ{111} = 2/30.5εa2
If a=1, ε=1
γ{100} = 4
γ{110} = 3.52
γ{111} = 1.16

## Slide 10
According to Eqn (1), the lower Miller index facets have low surface energy. System is stable only when it is in a state with the lowest Gibbs free energy. Therefore, a crystal is often surrounded by low index surfaces.
http://cmacd.myweb.cs.uwindsor.ca/Teaching/553-class/59-553_Notes3.pdf
http://chemistry.bd.psu.edu/jircitano/Miller.html
Notes: Miller Indices
Miller Indices
Rules for Miller Indices: Determine the intercepts of the face along the crystallographic axes, in terms of unit cell dimensions.
Take the reciprocals
Clear fractions
Reduce to lowest terms
For example, if the x-, y-, and z- intercepts are 2, 1, and 3, the Miller indices are calculated as: Take reciprocals: 1/2, 1/1, 1/3
Clear fractions (multiply by 6): 3, 6, 2
Reduce to lowest terms (already there)
Thus, the Miller indices are 3,6,2. If a plane is parallel to an axis, its intercept is at infinity and its Miller index is zero. A generic Miller index is denoted by (hkl).
If a plane has negative intercept, the negative number is denoted by a bar above the number. Never alter negative numbers. For example, do not divide -1, -1, -1 by -1 to get 1,1,1. This implies symmetry that the crystal may not have!
Some General Principles
If a Miller index is zero, the plane is parallel to that axis.
The smaller a Miller index, the more nearly parallel the plane is to the axis.
The larger a Miller index, the more nearly perpendicular a plane is to that axis.
Multiplying or dividing a Miller index by a constant has no effect on the orientation of the plane
Miller indices are almost always small.
Why Miller Indices?
Using reciprocals spares us the complication of infinite intercepts.
Formulas involving Miller indices are very similar to related formulas from analytical geometry.
Specifying dimensions in unit cell terms means that the same label can be applied to any face with a similar stacking pattern, regardless of the crystal class of the crystal. Face 111 always steps the same way regardless of crystal system.
Movie of aminated gif above. Click the pause button, then step through the planes

## Slide 11: Surface energy reduced by
Surface relaxation: surface atoms or ions shift inwardly.
Surface restructuring through combining surface dangling bonds into strained new chemical bonds
Surface adsorption through chemical or physical adsorption of terminal chemical species by forming chemical bonds or weak attraction forces such as electrostatic or van der Waals forces.
Composition segregation or impurity enrichment on the surface through solid-state diffusion.

## Slide 12: Surface energy reduction by surface relaxation

## Slide 13: Surface energy reduction by restructuring
The restructured {100} faces have the lowest surface energy among {111}, {110} and {100} faces.

## Slide 14: Surface energy reduction by chemical or physical adsorption

## Slide 15: Reduction of surface energy for a nanoparticle:
One is to reduce the total surface area. That is, surface tends to become spherical.
For crystalline particle, facets forms because they have smaller surface energy than a spherical surface does. Since facets with a lower Miller Index have a lower surface energy than that with a higher Miller Index. Therefore, crystal is often surrounded by low index surfaces.

## Slide 17
Wulff plot: using γi = Chi where C is the constant and hi is the perpendicular distance.

## Slide 18: Crystal Grown with Nonfacets
At certain high temperature, the equilibrium crystal surfaces may not be smooth, and difference in surface energy of various crystal facets may disappear. Such a transition is called surface roughening or roughening transition. Most nanoparticles grown at elevated temperature are spherical in shape (not facets).
Kinetic factors (processing or crystal growth conditions) may also prevent formation of facets.

## Slide 19: Mechanisms for reduction of overall surface energy
Combining individual nanostructures together to form large structures so as to reduce the overall surface area, which includes:
Sintering: individual structures merge together which occurs at 70% of Tm. Replacing solid-vapor interface by solid-solid interface and becomes polycrystalline.
Ostwald ripening: A large one grows at the expense of the smaller one until the latter disappears completely, and becomes a single crystal. It occurs at relatively low temperature.
Agglomeration of individual nanostructures through chemical bonds and physical attraction forces at interfaces without altering the individual nanostructures. The smaller the particles, the greater the bonding forces are.

## Slide 20: Thermodynamic potentials
Thermodynamic potentials are state functions that, together with the corresponding equations of state, describe the equilibrium behavior of a system as a function of so-called ”natural variables”. The natural variables are a set of appropriate variables that allow to compute other state functions by partial differentiation of the thermodynamic potentials.
Source: https://itp.uni-frankfurt.de/~gros/Vorlesungen/TD/5_Thermodynamic_potentials.pdf

## Slide 21: Review
The Laws of Thermodynamics
https://www.youtube.com/watch?v=8N1BxHgsoOw
Thermodynamic Potentials Part 2
https://www.youtube.com/watch?v=VVDaR6oczJU
Thermodynamic Potentials Part 1
https://www.youtube.com/watch?v=EgbrBJ3-OH4

## Slide 22: Thermodynamic equations
Internal Energy
Helmotz Free Energy
Enthalpy
Gibbs Free Energy
Landau
Potential
Where: T= temperature, S= enthropy, P= pressure, V=Volume, Ni is the number of particles and m is the chemical potential
Name
Formula
Fundamental equations
Variables
(depends on the system)

## Slide 23
Helmholtz free energy is often represented by F (particularly in physics), although IUPAC prefers the symbol A (which is used primarily in chemistry).
It can be shown that the knowledge of one of the thermodynamic potentials based on their natural variables allows obtaining all the thermodynamic variables of the system. This is possible by using the four Maxwell relationships for thermodynamics, partial derivative equations that relate state variables to thermodynamic potentials.
Each thermodynamic potential, under this point of view, is not only a physical quantity to which a value (real number) that we can eventually measure, but more properly must be seen as a mathematical functional dependence, which contains all the information of the system.
This is why we talk about the "natural variables" of each potential: they are the magnitudes that play the role of independent variables in the function associated with the potential

## Slide 24: Chemical Potential and Surface Tension
NOTE: Here Omega is the atomic volume not the Landau Potential
NOTE: Miu is the chemical potential
gamma is the surface energy
n is the number of particles
Flat surface
Migration of chemical species from a flat surface to a spherical particle
Similar to the Young-Laplace eqn
(1)

## Slide 25: Chemical Potential and Surface Tension
Flat surface
Evaporation of an atom form from a flat surface to the environment
Flat surface
Evaporation of an atom form from a flat surface to the environment
Chemical potential of the flat surface
Chemical potential of the convex surface
Pc is the equilibrium vapor pressure of the curved surface
Pinfinte is the equilibrium vapor pressure of the flat surface
If we combine with equation 1 from the previous slide:
Dm=
For a spherical particle
The vapor pressure of the particle increases as the radius of the particle
decreases

## Slide 26: Chemical potential and its effect on vapor pressure
Chemical potential and its effect on solubilty
Similarly, for solubility:
Sc
S∞
Let us discuss these behaviors

## Slide 27
Modeling size effects on the surface free energy of metallic nanoparticles and nanocavities
Shiyun Xiong,a Weihong Qi,*ab Yajuan Cheng,a Baiyun Huang,c Mingpu Wangab and Yejun Lia ; Physical Chemistry Chemical Physics Journal, Issue 2, 2011
https://pubs.rsc.org/en/content/articlelanding/2011/cp/c0cp02102d#!divAbstract
Notes: Abstract
Based on the rigorous consideration of the bond broken rule and surface relaxation, a model for the size-dependent surface free energy of face-centered-cubic nanoparticles and nanocavities is presented, where the surface relaxation is calculated by the BOLS relationship. It is found that the surface free energy of nanoparticles and nanocavities represents a reverse size effect—the surface free energy of nanoparticles decreases with the decrease of particle size while it rises with the shrinkage of cavities. The size effect on the surface free energy of nanoparticles and nanocavities is not evident in large size ranges, while it becomes more and more distinct with decreasing size, especially for sizes smaller than 10 nm. The present predictions are in good agreement with the available literature data.

## Slide 28: Ostwald Ripening Phenomenon

## Slide 29: Surface stress and surface energy of Al nanoclusters computed based on DFT calculation. The surface energy/stress-particle radius curves were drawn based on the data presented in ref. 29.
Wu, Jianbo & li, Panpan & Pan, Yung-Tin & Warren, Steven & Yin, Xi & Yang, Hong. (2012). ChemInform Abstract: Surface Lattice-Engineered Bimetallic Nanoparticles and Their Catalytic Properties. Chemical Society reviews. 41. 10.1039/c2cs35189g.
Notes: Abstract
When nanoparticles become small (ca. <5 nm), surface stress becomes significant and generates strain that results in a change of surface structures. In this regard, the surface lattice of nanoparticles can be engineered to create strains or other structural changes with atomic positions away from the normal lattice points. Such changes impact the electronic and catalytic properties of nanoparticles. Recently, several groups have reported the change of catalytic and electrocatalytic properties of bimetallic nanoparticles. In this tutorial review, we discuss the principles related to lattice strain and other distorted structures, and the catalytic properties of bimetallic nanostructures.

## Slide 30: Paper for Discussion
Surface Tension, Surface Energy, and Chemical Potential Due to Their Difference
https://pubs.acs.org/doi/abs/10.1021/la400937r

## Slide 31: Electric potential at the proximity of solid surface

## Slide 32: Interactions between 2 particles : DLVO Theory

## Slide 33: Interactions between 2 particles : DLVO Theory

## Slide 34: Steric stabilization: solvent and polymer

## Slide 35: Steric stabilization: solvent and polymer

## Slide 36: Steric stabilization: solvent and polymer

## Slide 37: Steric stabilization: mixed steric and electric interactions