## Slide 1: Soft matter, colloids and self-assembly to create mesoporous materials
February 24, 2020

## Slide 2: Soft /Condensed Matter
The phrase “soft matter” was used by Pierre de Gennes as the title of his 1991 Nobel Prize acceptance speech.
Refers to condensed matter that exhibits characteristics of both solids and liquids
Soft matter can flow like liquids (measurable viscosity)
Soft matter can bear stress (elastic deformation)
Viscoelastic behaviour = viscous + elastic
Examples: rubbers, gels, pastes, creams, paints, soaps, liquid crystals, proteins, cells

## Slide 3: Soft Matter
Soft matter does not exhibit the crystalline order that is characteristic of most hard matter (except amorphous solids).
Nevertheless, some order remains. Soft matter lends itself to self-assembly which produces a large variety of nanostructures.
Pierre-Gilles de Gennes received the 1991 Physics Nobel Prize for bringing order into soft matter, particularly liquid crystals and polymers.

## Slide 4
Phase diagram of water
Image: http://wps.prenhall.com/wps/media/objects/602/616516/Chapter_10.html

## Slide 5
What is Condensed Matter?
“Condensed matter” refers to matter that is not in the gas phase but is condensed as a liquid or solid. (condensed denser!)
Matter condenses when attractive intermolecular bond energies are comparable to or greater than thermal (i.e. kinetic) energy ~ kT.
Phase diagram of carbon dioxide
Image: http://wps.prenhall.com/wps/media/objects/602/616516/Chapter_10.html

## Slide 6: Soft matter
Types
Colloids
Polymers
Liquid Crystals

## Slide 7: Four characteristics of Soft Matter
Length scales
- Structures of ≈10-1000 nm determine the properties
Time scales: processes from 10-12 - 103 s
- Dynamics processes over a wide time scales 10-12 - 103 s
- Very slow processes in non-equilibrium configurations
Weak interactions
- Interactions between molecules and molecular structures ≈ kT
Self assembly
- Hierarchical arrangement of structures
- Competition between interaction energy and entropy

## Slide 8: Typical Length Scales
Atomic spacing: ~ 0.1 nm = 1A0
“Pitch” of a DNA molecule: 3.4 nm
Diameter of a surfactant micelle: ~6-7 nm
Gyration radius of a polymer molecule: ~10 nm
Diam. of a colloidal particle (e.g. in paint): ~200 nm
Bacteria cell: ~2 mm
Diameter of a human hair: ~80 mm

## Slide 9
Thermal fluctuations
Soft condensed matter is not static but in constant motion at the level of molecules and particles.
The “equipartition of energy” means that for each degree of freedom of a particle to move, there is 1/2kT of thermal energy.
For a colloidal particle able to undergo translation in the x, y and z directions, thermal energy is 3/2 kT.
k = 1.38 x 10-23 JK-1, so kT = 4 x 10-21 J per molecule at room temperature (300 K).
kT is a useful “gauge” of bond energy.
Vx
Vy
Vz
V
The kinetic energy for a particle of mass, m, is 1/2 mv2 = 3/2 kT. When m is small, v becomes significant.

## Slide 10
The importance of thermal fluctuations and Brownian motion
Thermal fluctuations of Soft Matter
Brownian motion can be though of as resulting from a slight imbalance of momentum being transferred between liquid molecules and a colloidal particle.
https://www.youtube.com/watch?v=PzssJDZn9xI

## Slide 11: Colloids

## Slide 12: Colloids
A colloid has sub-mm particles (but not single molecules) of one phase dispersed in a continuous phase.
The size scale of the dispersed phase is between 1 nm and 1 mm.
The dispersed phase and the continuous phase can consist of either a solid (S), liquid (L), or gas (G)
There is no “gas-in-gas” colloid, because there is no interfacial tension between gases!
Dispersed Phase | Continuous Phase | Name | Example
L/S | G | aerosol | Fog, hair spray, smoke
G | L/S | foam | Beer froth, shaving foam
L | L/S | emulsion | Mayonnaise, salad dressing
S | L | sol | Latex paint, tooth paste
S | S | solid suspension | Pearl, mineral rocks

## Slide 13
Interfacial Area of Colloids
r
For a spherical particle, the ratio of surface area (A) to volume (V) is:
Thus, with smaller particles, the interface becomes more significant. A greater fraction of molecules is near the surface.
Consider a 1 cm3 phase dispersed in a continuous medium:
No. particles Particle volume(m3) Edge length (m) Total surface area(m2)
1 10-6 10-2 0.0006
103 10-9 10-3 0.006
106 10-12 10-4 0.06
109 10-15 10-5 0.6
1012 10-18 10-6 6.0
1015 10-21 10-7 60
1018 10-24 10-8 600

## Slide 14: Mesoporous Materials

## Slide 15: Outline
What are they?
What are they useful for?
What are some of the theoretical aspects behind these materials?
How can we synthetize them?
What are the factors affecting their sizes, shapes and their existence ?

## Slide 16: What are mesoporous materials?
Porous materials whose pores are between 2 and 50 nm in diameter.
The mesoporous materials investigated here have uniformly ordered pores.
Silica based materials first synthesized by scientists at the Mobil Corporation in 1992.
Non-silica mesoporous materials first reported at UC Santa Barbara in 1994.

## Slide 17: Applications
Molecular sieves
High surface area catalysts
Gas sensors
Dye sensitized photovoltaic solar cells
0-Dimension nano-particles

## Slide 18: Mesoporous materials are templated by amphiphilic molecules.
An amphiphillic molecule has a hydrophillic (water loving) head and a hydrophobic (water loathing) tail.
Surfactant is an amphiphilic molecule with a tendency to adsorb onto free surfaces and interfaces and to aggregate to form micelles
A micelle is an association of amphiphillic molecules.
Mesoporous structures are created by the ordered packing of micelles.
Small molecules Mw≈100-1000
Courtesy of Brian Eggiman

## Slide 19: Why do amphiphiles form micelles?
Gibb’s Free Energy (ΔG) is a thermodynamic quantity which predicts the spontaneity of a reaction. (A decrease in Gibb’s Free Energy indicates a spontaneous reaction)
Water molecules create structure by forming hydrogen bonds with one another.
The hydrophobic tails of individual amphiphiles placed in solution force water molecules to associate in a particular way. This decreases the entropy (ΔS) of the system.
When the hydrophobic tails associate to each other (form micelles) in order to minimize their interaction with water molecules they increase the entropy of the system.
ΔG = ΔH - TΔS
An increase in entropy, decreases Gibb’s Free Energy of the system therefore the reaction will occur spontaneously.

## Slide 20
Examples of Self-Assembly
Surfactants can assemble into (a) spherical micelles, (b) cylindrical micelles, (c) bi-layers (membranes), or (d) saddle surfaces in bicontinuous structures
From I.W. Hamley, Introduction to Soft Matter
(a)
(b)
(c)
(d)

## Slide 21: Examples of Self-Assembly
Surfactants can create a bi-continuous surface to separate an oil phase and a water phase.
The hydrophilic end of the molecule orients itself towards the aqueous phase.
The oil and water are completely separated but both are CONTINUOUS across the system.
From RAL Jones, Soft Condensed Matter
The “plumber’s nightmare”

## Slide 22
Colloidosomes: Self-assembled colloidal particles
A.D. Dinsmore et al., “Colloidosomes: Selectively Permeable Capsules Composed of Colloidal Particles,” Science, 298 (2002) p. 1006.
Liquid B
Liquid A
Colloidal particles (<1 mm)

## Slide 23
MRS Bulletin,
Feb 2004, p. 86
Colloidal Crystals
Colloidal particles can have a +ve or -ve charge.
In direct analogy to salt crystals of +ve and -ve ions, charge attractions can lead to close-packing in ordered arrays.

## Slide 24: What determines micelle shape?
Diagrams compiled from work by Brian Eggiman and Soler-Illia et al, “Chemical Strategies To Design Textured Materials: from Microporous and Mesoporous Oxides to Nanonetworks and Hierarchical Structures”, Chem. Rev. 2002, 102, 4093-4138.

## Slide 25: Transition from dispersed state to condensed state: a universal phenomenon Beginning of self-assembly of molecules, polymers, or microscopic particles
Gas (dispersed)  Liquid (condensed)
under van der Waals attraction forces
(b) Polymer gels (dispersed)  Collapsed polymer gel (condensed)
under rubber elasticity (entropy change), counter ions osmotic pressure, and electrostatic repulsive forces
(c) Colloidal particles (dispersed)  self-assembled colloidal crystals and super lattice structures

## Slide 26: Surfactants and Amphiphilic Molecules
Surfactant characteristics: Head group charge, chain length, head group size
Cationic:
long chain amines or ammonium salts are positively charges at pH<7,
not charged at pH >7, then not active
quaternary ammonium salts are charged and active at all pH’s
Anionic:
Long chain carboxylic or sulfonic acids, are negatively charges at pH > 7,
(at pH < 7 not ionized, not active)
Surfactant Activity depends on:
pH, ionic strength of the solution and by counter ions
Counter ions neutralize charges on surfactant head groups, and even cause its precipitation.
Non-ionic surfactants have the advantage in that pH, counter ions, or solvents do not affect their activity.

## Slide 27: Surfactants and amphiphiles
Amphiphilic molecule: two parts with very different affinities
Ex: hydrophilic head and hydrophobic tail

## Slide 28: Critical Micelle Concentration
f - volume fraction of amphiphile
< fc – monomers
f > fc - micelles of average size M
fc = exp(-∆e/kBT) (CMC)

## Slide 29: Packing Geometry: Attaining the Desired Self-Assembled Structures
Structure depends on pH, T, electrolyte concentration
Major driving forces for amphiphyles to form well-defined aggregates are:
hydrophobic attraction at hydrocarbon-water interfaces and
hydrophilic ionic or steric repulsion between head groups.
Geometric packing parameter
(shape factor)
v = hydrocarbon chain volume
a0 = optimal head group area
lc = critical chain length
> 1 | > 0.5 | < 0.5 | R
inverse micelle | bilayers | spherical-cylindrical | structure

## Slide 30: Packing Geometry: Attaining the Desired Self-Assembled Structures at Constant Temperature
Spherical Micelles
Lamellar Phase
Cubic Phase
Reverse Micelles
Hexagonal Phase
Rod-like Micelles
Increase Surfactant Conc.: spherical micelles rod-like micelles  cubic  lamellar

## Slide 31: Packing Geometry: Attaining the Desired Self-Assembled Structures vs. Temperature
T

## Slide 32: Packing Geometry: Attaining the Desired Self-Assembled Structures considering Physico-Chemical aspects
Effect of surfactant concentration
Surfactant conc ↑: lower hydration of head groups →
lower a0 → higher R → lamellar structure
Effect of surfactant chain length
If lc increases, v increases, however if R increases too much, spherical → lamellar
Effect of co-solvent
Polar solvents, like alcohols, tend to associate with head groups and reduce the tendency for the surfactant molecules to associate; CM may disappear,
Non-polar solvents associate with hydrophobic chains of the surfactant increase v → increase R → less curved structures
Effect of salts and ionic species
On ionic surfactants, reduces repulsive energy between head groups, reducing a0 → larger R → less curved structures

## Slide 33: Shape of aggregates
Basic shapes:
spheres
cylinders
bilayers
vesicles
Superstructures:
micellar crystals
lamellar phases
bicontinuous networks
- …
Self assembled structures are rich in phases:
response by changing size and shape and arrangement of micelles
dramatic change in properties

## Slide 34: Shape of aggregates
Factors determining the shape
Optimum head group are, a0
Critical chain length, lc
Hydrocarbon volume, v
lc - length of fully extended tail
v - volume of the tail
# of tails, side groups, …
v
lc

## Slide 35: Optimum head group area, a0
a0 controlled by
repulsive forces:
electrostatic or steric repulsion
(can be altered by e.g
salt concentration)
attractive forces:
protecting the tail

## Slide 36: Shape of aggregates
Spheres - smallest area/volume
Volume:
4p r3/3=Nv
(N is the # of molecules in aggregate)
Surface area:
4p r2=Na0
-> r = 3v/a0
but rmax ≤lc
v/lca0 ≤ 1/3 for spherical micells

## Slide 37: Shape of aggregates
Spheres:
v/lca0 ≤ 1/3
Cylinders:
1/3≤ v/lca0 ≤ 1/2
Bilayer:
v/lca0 > 1/2

## Slide 38: Spherical micelles
Spheres formed when:
v/lca0 ≤ 1/3
Size of micelles finite ->
eN has a minimum value at an optimum number M
XN - volume fraction of micelles
with N molecules
size distribution

## Slide 39: Packing Geometry: Attaining the Desired Self-Assembled Structures

## Slide 40: Macro vs. micro phase separation
Simple liquids (water & oil):
free energy when a molecule joins an aggregate
N - number of molecules in the aggregate
g - interfacial energy, v - molecular volume
eN - monotonic decreasing function of N
-> infinite aggregates - macroscopic phase separation
Amphiphiles:
-> finite size of aggregates - microscopic phase separation
Why?

## Slide 41: Macro vs. micro phase separation
Amphiphiles:
-> micro-phase separation
-> finite size of aggregates
-> entropic considerations more important
Why? Balance between protecting the hydrophobic tail
and keeping the head in contact with the water
associating tails vs. repulsion of head groups

## Slide 42: Cylindrical micelles
Spheres formed when:
1/3<v/lca0 ≤ 1/2
Size of micelles finite but
eN has a no minimum -
energy of a molecule in the
cylinder is independent of
the size -> only 2∆Eend
-> forming larger micelles leads to energy gain, but a loss in entropy

## Slide 43: Bi-layers

## Slide 44: Bilayers
Bilayers formed when:
v/lca0 > 1/2
∆Eedge(A)  A1/2 (A - area of a layer)
dependent on the size of the bilayer
-> formation of infinite layers
Vesicles - closed surface by a bilayer
-> model for cell membranes
-> drug delivery systems
-> colloidal behaviour

## Slide 45: Bilayers
Cell membranes - phospholipid bilayers
Two tails give a large volume, v
v/lca0 > 1/2

## Slide 46: Bilayers
Bilayers are not flat - highly crumpled
Persistence length:
k - bending modulus of membrane
For r > x direction in membrane is lost
Lamellar phases can anyway be obtained
with very large d -> confinement between
two adjacent planes leads to loss in entropy

## Slide 47: Bilayers
Lamellar phase can be distorted by fluctuations
forming complex geometries

## Slide 48: Phase behaviour
Self assembled structures are rich in phases
-> response by changing size and shape and arrangement of micelles
-> dramatic change in properties

## Slide 49: Phase behaviour
Self assembled structures are rich in phases
-> response by changing size and shape and arrangement of micelles
-> dramatic change in properties

## Slide 50
Micelles and Inverse Micelles
Surfactant: Hydrophilic Head Example: Phospholipid
+ Hydrophobic Tail
Micelle: Inverse Micelle:
Heads outside, Water outside Heads inside, Water inside

## Slide 51
Bilayer Structures
, Vesicle
Part of a Cell Wall

## Slide 52
Drug Delivery via Liposomes

## Slide 53
Supramolecular Assemblies

## Slide 54
Notes: This overview figure demonstrates the large variety of ways to mimic life in artificial nanostructures. It is taken from a highly popular study of the National Academy of Sciences which quickly went out of print. A 2008 follow-up study can be found at http://sites.nationalacademies.org/bpa/BPA_048192 .

## Slide 55: Competitions on Self-Assembly

## Slide 56: Competitions in Self-Assembly
Molecules often segregate at an interface to LOWER the interfacial energy - leading to an ordering of the system.
This self-assembly is opposed by thermal motion that disrupts the ordering.
Self-assembly usually DECREASES the entropy, which is not favoured by thermodynamics.
But there are attractive and repulsive interactions between molecules that dominate.
DF = DU - TDS
If free energy decreases (DF < 0), then the process is spontaneous.
Entropy (S) increase is favourable
Internal Energy (U) decrease is favourable

## Slide 57: Importance of Interfaces
Free energy change: dF = GdA
An increase in area raises the system’s free energy, which is not thermodynamically favourable.
So, sometimes interfacial tension opposes and destroys self-assembly.
An example is coalescence in emulsions.

## Slide 58
Coalescence in Emulsions
Surface area of N particles: 4 N p r2
Surface area of droplet made from coalesced droplets: 4 p R2
Liquid droplet volume before and after coalescence:
R
r
Change in area, DA = - 4pr2(N-N2/3)
In 1 L of emulsion (50% dispersed phase), with a droplet diameter of 200 nm, N is ~ 1017 particles. Then DA = -1.3 x 104 m2
With G = 3 x 10-2 J m-2, DF =GDA = - 390 J.

## Slide 59
I. Karakurt et al., Langmuir 22 (2006) 2415
Hydrophilically-driven self-assembly of particles

## Slide 60: Synthesis of Mesoporous Materials

## Slide 61: How do we use micelles to form mesoporous metal oxides?
Courtesy of Brian Eggiman

## Slide 62: Self-assembled Block Copolymer Nanostructures
Block copolymers are amphiphilic molecules containing distinctively different polymer segments (blocks):
polystyrene (H (C6H5 – CH2 – CH) - ) + poly isoprene (-CH2 – H3 (CH=CH2)C - ) block
polystyrene and poly butadiene (- CH-CH=CH-CH) - ) block copolymer
(-CH2-CH2-) polyethylene and poly propylene (-(CH2-CH3CH)-) block copolymer
polyUrethane (-(CH2-CH2-O2C-NH-C6H10CH2-C6H10-NH-OC)-)+polyUrethane block copolymer
Different blocks in a single polymer chain are covalentely bonded.
The phase separation occurs on the nanometer scale, as determined by the dimension of the blocks.
Factors: monomer type, composition and molecular size, and molecular configuration.

## Slide 63: 2.5 Self-assembled Block Copolymer Nanostructures

## Slide 64: 2.5 Self-assembled Block Copolymer Nanostructures
Flory-Huggins segment-segment interaction parameter X:
phase separation is favored
E: Interaction Energy
f = volume fraction
fA = fB → straight cylinder → lamellar phase
fA > fB → cone structure → B phase dispersed in A phase as spherical micelles
fB > fA → cone structure → A phase dispersed in B phase as spherical micelles

## Slide 65: 2.6Co-Assembly of Liquid Structures and Inorganic Materials
Self-assembled liquid crystals from surfactants act as a template to support the growth of ceramic materials. These ordered structures are cross-linked together through the condensation of the aluminosilicate ions. Subsequently, the surfactant molecules can be removed by thermal or chemical treatment without collapsing the ordered structure (2-50 nm tunable).
Self-assembled periodic structures can be further used as a structural frame work to develop new materials:
by incorporating functional molecules and active sites into the porous channels (e.g. nanoporous silica)
by using the periodic nanoporous structures as a template (e.g. for carbon or metals)
by physically confining a new material in the organized nanostructures.

## Slide 66: Co-Assembly of Liquid Structures and Inorganic Materials
Interactions between cationic surfactants and Anionic Silicates
Mesoporous materials: mixing aluminosilicate precursors (e.g. sodium aluminate, tetramethyl ammonium silicate, and silica) in a surfactant solution (e.g. ≥ 1 wt% cetyltrimethyl ammonium bromide (CTAB))
Inorganic ions play an important role in the self assembly process

## Slide 67
Materials with controlled structure obtained through self-assembly
Micelles are packed together
SiO2 (silica) is grown around the micelles
Micelles are removed to leave ~ 10 nm spherical holes. Structure has low refractive index. Can be used as a membrane.
P. Ball, Nanotechnology (2002) 13, R15-R28

## Slide 68: Langmuir-Blodgett Films
Definition of LB films
  History and development
Construction with LB films
Building simple LB SAMs
Nano applications of LB films
  Surface derivatized nanoparticles
  Functionalized coatings in LB films

## Slide 69: Langmuir-Blodgett Films
A Langmuir-Blodgett film contains of one or more monolayers of an organic material, deposited from the surface of a liquid onto a solid by immersing (or emersing) the solid substrate into (or from) the liquid. A monolayer is added with each immersion or emersion step, thus films with very accurate thickness can be formed. Langmuir Blodgett films are named after Irving Langmuir and Katherine Blodgett, who invented this technique. An alternative technique of creating single monolayers on surfaces is that of self-assembled monolayers. Retrieved from "http://en.wikipedia.org/wiki/Langmuir-Blodgett_film"

## Slide 70: Langmuir-Blodgett Films
http://www.ksvltd.com/pix/keywords_html_m4b17b42d.jpg
Deposition of Langmuir-Blodgett molecular assemblies of lipids on solid substrates.
http://www.bio21.bas.bg/ibf/PhysChem_dept.html

## Slide 71: Self Assembly
Self-assembly is the fundamental principle which generates structural organization on all scales from molecules to galaxies. It is defined as reversible processes in which pre-existing parts or disordered components of a preexisting system form structures of patterns. Self-assembly can be classified as either static or dynamic.
http://en.wikipedia.org/wiki/Self-assembly

## Slide 72: Molecular Self-Assembly
Molecular self-assembly is the assembly of molecules without guidance or management from an outside source. There are two types of self-assembly, intramolecular self-assembly and intermolecular self-assembly, although in some books and articles the term self-assembly refers only to intermolecular self-assembly. Intramolecular self-assembling molecules are often complex polymers with the ability to assemble from the random coil conformation into a well-defined stable structure (secondary and tertiary structure). An example of intramolecular self-assembly is protein folding. Intermolecular self-assembly is the ability of molecules to form supramolecular assemblies (quarternary structure). A simple example is the formation of a micelle by surfactant molecules in solution.
http://en.wikipedia.org/wiki/Self-assembly

## Slide 73: Self Assembled Monolayers
SAMs – Self Assembled Monolayers
Alkane Thiol complexes on gold
  C10 or longer, functionalized end groups
Can build multilayer / complex structures
Used for creating biosensors
  Link bioactive molecules into a scaffold
The first cells on earth formed from SAMs

## Slide 74: The Self-Assembly Process
The self-assembly process. An n-alkane thiol is added to an ethanol solution (0.001 M). A gold (111) surface is immersed in the solution and the self-assembled structure rapidly evolves. A properly assembled monolayer on gold (111) typically exhibits a lattice.
A schematic of SAM (n-alkanethiol CH3(CH2)nSH molecules) formation on a Au(111) sample.

## Slide 75: SAM Technology Platform
SAM reagents are used for electrochemical, optical and other detection systems. Self-Assembled Monolayers (SAMs) are unidirectional layers formed on a solid surface by spontaneous organization of molecules.
Using functionally derivatized C10 monolayer, surfaces can be prepared with active chemistry for binding analytes.
http://www.dojindo.com/sam/SAM.html

## Slide 76: Surface Contamination
All surfaces become contaminated!
It is a form of ‘passivation’
  Oxidation of metals
  Adventitious hydrocarbons
  Chemisorption of ions
It can happen very rapidly
And be very difficult to remove

## Slide 77: Surface Treatments
Control friction, lubrication, and wear
Improve corrosion resistance (passivation)
Change physical property, e.g., conductivity, resistivity, and reflection
Alter dimension (flatten, smooth, etc.)
Vary appearance, e.g., color and roughness
Reduce cost (replace bulk material)

## Slide 78: Surface Treatment of NiTi
Biomedical Devices and Biomedical Implants – SJSU Guna Selvaduray

## Slide 79: Surface Treatment of NiTi
XPS spectra of the Ni(2p) and Ti(2p) signals from Nitinol undergoing surface treatments show removal of surface Ni from electropolish, and oxidation of Ni from chemical and plasma etch. Mechanical etch enhances surface Ni.
Biomedical Devices and Biomedical Implants – SJSU Guna Selvaduray

## Slide 80: Surfaces in Nature
Cell membranes
  Self-assembled phospholipid bilayers
  Proteins add functionality to the membrane
Skin (ectoderm)
Lungs
  Exchange of O2, CO2, and water vapor
Cell surface recognition (m-proteins)
  Major histocompatibility complex

## Slide 81: Molecular Self Assembly
3D diagram of a lipid bilayer membrane - water molecules not represented for clarity
http://www.shu.ac.uk/schools/research/mri/model/micelles/micelles.htm
Different lipid model
top : multi-particles lipid molecule
bottom: single-particle lipid molecule

## Slide 82: Cell Membranes
http://faculty.clintoncc.suny.edu/faculty/Michael.Gregory/default.htm

## Slide 83: Physical chemistry of solid surfaces

## Slide 84: Surface
Nanostructures and nanomaterials possess a large fraction of surface atoms per unit volume.
  For a cube of iron of 1 cm3 the % of surface atoms would be only 10-5%.
  For a cube of iron of 1000 nm3 the surface atoms would increase to 10%.
This explain why changes in the size range of nanometers are expected to lead to great changes in the physical and chemical properties of the materials.

## Slide 85: The total surface energy increases with the overall surface area
For 1gr of NaCl
When the particles change from centimeter size to nanometer size, the surface area and the surface energy increases seven orders of magnitude

## Slide 86: Important
All nanostructured materials possess a huge surface energy.
They are thermodynamically unstable or metastable.
It is necessary to overcome the surface energy, and to prevent the nanostructures or nanomaterials from growth in size, driven by the reduction of overall surface energy.

## Slide 87: Surface energy
Origin
  Atoms or molecules on a solid surface possess fewer nearest neighbors or coordination numbers, thus have unsatisfied bonds exposed to the surface.
  The lattice constants of the entire solid particles show an appreciable reduction.

## Slide 88: When there is an appreciable surface relaxation such as the surface atoms moving inwardly, or there is a surface restructuration, surface energy will be lower than that estimated by this equation.
Definition
  It is the energy required to create a unit area of “new” surface
surface area
half of the bond strength
Number of atoms/unit area
number of broken bonds
when brake into two pieces

## Slide 90: There is a strong tendency to minimize the total surface energy
  Surface relaxation. The surface atoms or ions shift inwardly which occur more readily in liquid phase than in solid surface due to rigid structure in solids. This would result in a reduction of the surface energy.

## Slide 91: Mechanisms to minimize the total surface energy
  Surface restructuring through combining surface dangling bonds into strained new chemical bonds.

## Slide 92
  Surface energy of (100) faces in diamond and silicon crystals before restructuring is higher than both (111) and (110) faces.
  However, restructured (100) faces have the lowest surface energy among three low indices faces, and such surface restructuring can have a significant impact on the crystal growth.

## Slide 93: Mechanisms to minimize the total surface energy
  Through chemical or physical adsorption of terminal chemical species onto the surface by forming chemical bonds or weak attraction forces such as electrostatic or van der Waals forces

## Slide 94: Mechanisms to minimize the total surface energy
  Composition segregation or enrichment of impurity on the surface through solid-state diffusion.
  In nanostructures and nanomaterials phase segregation may play a significant role in the reduction of surface energy, considering the great impact of surface energy and the short diffusion distance.

## Slide 95: At the individual nanostructure level, there are two approaches to the reduction of the total surface energy
Reduce the overall surface.
  For liquid and amorphous solids, spherical shape
    Water on a hydrophobic surface
    Hot glass
  For a crystalline solid different crystals facets possess different surface energy.
    A crystalline particle normally forms facets
    There is a minimal surface energy when a group of surfaces is combined in a certain pattern.

## Slide 96: Examples of single crystals with thermodynamic equilibrium shape. (Top-left) Sodium chloride,(top-right) silver, (bottom left) silver, and (bottom-right)gold.

## Slide 97: Morphology
Kinetic factors, which are dependent on the processing or crystal growth conditions.
Non equilibrium conditions.
Below certain temperature the crystal is faceted.
Most nanoparticles grown by solution methods at elevated temperatures are spherical in shape and do not form any facets.

## Slide 98: At the overall system level, mechanisms for reduction of overall surface energy include:
Combining individual nanostructures together to reduce the surface
  Sintering, in which individual structures merge together, 0.7Tm. (must be avoided)
  Ostwald ripening, in which relatively large structures grow at the expense of smaller ones.
Agglomeration of individual nanostructures without altering the individual nanostructures (should be prevented)

## Slide 99: Sintering & Ostwald ripening
Fig 2.9

## Slide 100: Measuring Surfaces
AFM – Atomic Force Microscopy (1)
SEM – Scanning Electron Microscopy (2)
XPS (ESCA) – X-Ray Photoelectron Spectroscopy (3)
AES – Auger Electron Spectroscopy (3)
SSIMS – Static Secondary Ion Mass Spectroscopy (4)
Laser interferometry/Profilometry (5)

## Slide 101: Summary
Surfaces are discontinuities
Surface area creates energy
Dangling bonds lead to passivation
Interfaces are critical to ‘bonding’
Surfaces can be modified / derivatized
Surfaces are critical to life
  All important things happen at a surface!