## Slide 1: Study of titanate nanotubes by X-ray and electron diffraction and electron microscopy
Objective
The structure of titanate nanotubes prepared by the hydrothermal method was identified to be related to the structure of NaxH2 − xTi2O5·H2O. This was approved by the comparison of powder X-ray diffraction pattern.
Samples
The investigated Ti-NT samples were prepared by hydrothermal treatment of nanocrystalline TiO2 anatase powder. The powder was dispersed in 10 M NaOH aqueous solution. This suspension was put into a closed vessel and heated at 120 °C for 48 h. After the synthesis, the sample was washed and neutralized by HCl. In order to obtain powder samples of Ti-NTs, the sample was freeze-dried.
Conclusion
For improving the agreement of the simulated and experimental X-ray diffraction patterns, it is suggested that the effect of preferred orientation of nanotubes on the substrate holder should be considered
Procedure
PXRD gives information on the crystalline structure averaged over irradiated volume. On the other hand, HRTEM can be used to visualize the structure of a single nanotube. One of the challenges of this study was to find the required single nanotube. Ti-NTs were ultrasonically dispersed in ethanol and then a drop of the sample was spread on a holey carbon-coated microscope copper grid. Individual nanotubes were studied by HRTEM imaging, performed on JEOL JEM 2100 F FEG (field emission gun) operated at 200 kV accelerating voltage